Technical Product Data sheet

Product Name: Highbuild Texture W/B

Product description: Water borne high build textured masonry coating formulated for trowel and roll application. Based on modified vinyl acrylic resin, Highbuild W/B exhibits excellent adhesion to most masonry surfaces and may be textured

using appropriate rollers to provide attractive finishes.

Uses:

Decoration and protection of a wide range of masonry surfaces and primed

exterior plywood.

Pack sizes availability:10 & 20 litres

Colour range: White plus standard colour card

Special colours on request subject to minimum batch sizes

Specific gravity: Approx 1.7

Flash point: Non flammable

Recommended Spreading rate: Approx. 1litre/m

Solids content: Approx 77% w/w. Approx 60% v/v

Drying time: Approx 4 hours 20°C 65%RH

Over-coating time: Approx 16hours 20°C 65%RH

Minimum application temperature: Air and surface temperature should be 5

°C and rising. Do not apply during damp or frosty weather or when rain is imminent

Recommended dry film thickness: Approximately 600 microns

Method of application: Brush, roller or airless spray

Preparation: Surfaces must be clean, sound and dryand prepared in accordance with BS6150 Painting of buildings –code of practice. Bare metal surfaces must be adequately primed.

Storage life: Min 12 months in original sealed containers. Protect from frost and direct heat

Thinning/cleaning: Thin where necessary with clean water.

Do not exceed 1 part water to 10 parts of Highbuild W/B.

Wash equipment immediately after use with water and detergent

Safety precautions: Refer to the safety data sheet before use

Volatile organic content (voc) Limit for this product: Cat A/c 40g/l (2010).

This product contains maximum 5g/l VOC

Disposal: As supplied or containing liquid product–non hazardous waste code

08 01 12 waste paint and varnish other than those mentioned in 08 01 11

Used containers drained/rigorously scraped out and containing only dry

residues: categorised as non-hazardous with waste code 15 01 02 (plastic package) and 15 01 04 (metal package)